D&C  DR:dh


SECTION 034816
PRECAST CONCRETE SPLASH COURSE

PART 1  GENERAL

1.01
SUBMITTALS


A.
Product Data:  Manufacturer's catalog cuts, specifications, and installation instruction.

1.02
QUALITY ASSURANCE


A.
Random freeze thaw test shall be conducted by the manufacturer.  Test specimens shall retain 60 percent of its initial modulus of elasticity after 300 cycles.  Furnish test results to the Director upon request.

PART 2  PRODUCTS

2.01
MATERIALS


A.
Precast Concrete:  Normal weight, air entrained concrete.  Air content shall be 6 percent by volume within an allowable tolerance of plus or minus 1.5 percent.



1.
Minimum Compressive Strength for Splash Blocks:  4000 psi.


B.
Bar Reinforcement:  ASTM A 615, Grade 60, deformed.

2.02
FABRICATION


A.
Splash blocks shall be cast at the manufacturer's plant, not at the job site.  Castings shall have plane smooth surfaces, true to line and face, free from defects and sharp arises.  Overall dimensions for castings shall not vary more than 1/16 inch from those indicated.

PART 3  EXECUTION

3.01
INSTALLATION


A.
Set splash blocks true to line and grade.  Grade all spaces to provide solid support for splash blocks.

END OF SECTION

Updated 07/07/2009

Printed 7/7/2009
034816 - 1
Project No. 


