D&C  WAF:smb


SECTION 321236
PAVEMENT SEALING

PART 1   GENERAL

USE ARTICLE BELOW IF PATCHING IS REQUIRED, EDIT SECTIONS AS REQUIRED FOR PATCHING.
1.01
RELATED WORK SPECIFIED ELSEWHERE


A.
Patching Existing Paving:  Section 320117.

1.02
SUBMITTALS


A.
Product Data:  Manufacturer’s catalog cuts, specifications, installation instructions for sealants.

1.03
PROJECT CONDITIONS


A.
Environmental Conditions:



1.
Do not apply sealant when the air temperature is 50 degrees F or lower and falling, when the pavement is wet, or when rain is anticipated within eight hours.


B.
Allow a minimum of 7 days to lapse, and follow manufacturer’s written instructions, before applying sealant to new asphalt surfaces.

PART 2   PRODUCTS

2.01
MATERIALS


A.
Sealant:  FS R-P-355d, “Pitch, Coal Tar Emulsion (Coating for Bituminous Pavements)”.

DELETE BELOW IF SAND FILLED COATING IS NOT REQUIRED.

B.
Mineral Aggregate:  Clean, hard and durable graded silica, free from deleterious matter such as clay, dirt, organic matter or mineral salts and conforming to the following gradations:

	SIEVE DESIGNATION
	PERCENT PASSING

	No. 16
	100

	No. 30
	15 - 85

	No. 50
	2 - 10

	No. 100
	0 - 2


PART 3   EXECUTION

3.01
PREPARATION


A.
Remove all dust, dirt, salt, paint, loose pavement markings, and other foreign matter.


B.
Scrape, burn, or wash with detergent solution to remove accumulations of oil or grease.  Flush away residue with clean water and allow to dry.

3.02
APPLICATION

DELETE BELOW IF SAND FILLED COATING IS NOT REQUIRED.

A.
Mix mineral aggregate with sealant to a smooth, uniform consistency at the following proportions.

	MINERAL AGGREGATE PER GALLON

	First Application
	3 - 6 pounds dry weight

	Second Application
	1 - 2 pounds dry weight



B.
Apply sealant by squeegee, brush, or mechanical equipment in accordance with the manufacturer’s printed instructions at the following rate:

	UNDILUTED GALLONS PER SQUARE YARD

	First Application
	.10 to .12

	Second Application
	.08 to .10



C.
Allow sealant to cure 24 hours prior to opening to traffic.

END OF SECTION

Updated 07/08/09

Printed 4/14/2015
321236 - 1
Project No. 


