SECTION 321313
PORTLAND CEMENT CONCRETE ROAD PAVING

PART 1   GENERAL

1.01
RELATED WORK SPECIFIED ELSEWHERE


A.
Earthwork:  Section 310000.

1.02
SUBMITTALS


A.
Quality Control Submittals:



1.
Data:  Name and location of batch plant for concrete paving.

USE PARAGRAPH BELOW WITH EPD REQUIREMENT WHEN PROJECT ESTIMATE IS $1M OR MORE.
B. 
Submit an Environmental Product Declaration (EPD) from the manufacturer for concrete this specification section, if available. A statement of the contractor’s good faith effort to obtain the EPD shall be provided if not available.

1. Manufacturer-provided EPDs must be Product Specific Type III (Third-Party Reviewed), in adherence with ISO 14025 Environmental labels and declarations, ISO 14044 Environmental management – Life cycle assessment, and ISO 21930 Core rules for environmental product declarations of construction products and services.

PART 2   PRODUCTS

2.01
MATERIALS


A.
Portland Cement:  DOT Section 701-01 Type 2 (ASTM 150).


B.
Concrete:  DOT Table 501-3, Class C.


C.
Wire Fabric for Concrete Reinforcement:  DOT Section 709-02.  (ASTM A 185).


D.
Premoulded Resilient Joint Filler:  DOT Section 705-07.  (ASTM D 1751).


E.
Transverse Joint Supports:  DOT Section 705-15.


F.
Joint Sealants:



1.
Longitudinal Joints:  705-10.



2.
Transverse Joints:  705-12.



3.
Lubricant (for joint sealants):  705-13.


G.
Curing Materials:



1.
Quilted Covers:  DOT 711-02.



2.
Plastic Coated Fiber Blankets:  DOT 711-03.  (ASTM C 171).



3.
Polyethylene Curing Covers:  DOT 711-04.  (ASTM C 171).



4.
Membrane Curing Compound:  DOT 711-05.

PART 3   EXECUTION

3.01
INSTALLATION


A.
Construct concrete pavement in accordance with DOT Section 502 Portland Cement Concrete Pavement.  Conform to the line, grade, and cross section indicated.

END OF SECTION

Updated 06/29/2023

Printed 6/29/2023
321313 - 2
Project No. 


