D&C  WAF:hf


SECTION 321614
PRECAST CONCRETE CURBS

PART 1   GENERAL

1.01
RELATED WORK SPECIFIED ELSEWHERE


A.
Earthwork:  Section 310000.

B.
Concrete Paving Joint Sealants:  Section 321373.

1.02
SUBMITTALS


A.
Product Data:  Catalog sheets, specifications, and installation instructions for precast curbs.

USE PARAGRAPH BELOW WITH EPD REQUIREMENT WHEN PROJECT ESTIMATE IS $1M OR MORE.
B. 
Submit an Environmental Product Declaration (EPD) from the manufacturer for concrete this specification section, if available. A statement of the contractor’s good faith effort to obtain the EPD shall be provided if not available.

1. Manufacturer-provided EPDs must be Product Specific Type III (Third-Party Reviewed), in adherence with ISO 14025 Environmental labels and declarations, ISO 14044 Environmental management – Life cycle assessment, and ISO 21930 Core rules for environmental product declarations of construction products and services.


C.
Quality Control Submittals:



1.
Test Reports:  Random freeze thaw tests shall be conducted by the manufacturer.  Test specimens shall retain 60 percent of its initial modulus of elasticity after 300 cycles.  Test results shall be made available to the Director upon request.

PART 2   PRODUCTS

2.01
MATERIALS


A.
Provide precast concrete curbs with a minimum compression strength of 5000 pounds per square inch.  Castings shall have plane smooth surfaces, true to line and face, free from defects, sharp arises, and with curved surfaces accurately reproduced.  Overall dimensions for each casting shall not vary more than 1/16 inch from those indicated.


B.
Curb units shall be cast at the manufacturers plant.  Job site castings will not be permitted.


C.
Curbing to be set on a radius of 100 feet or less shall be cast to the curve required.  Ends shall be formed or sawed on radial lines.


D.
Curb Foundation:  One part Portland cement to six parts No. 1A coarse aggregate dry mix.

PART 3   EXECUTION

3.01
INSTALLATION


A.
Set curb true to line and grade on a foundation of one cubic foot of dry concrete for each linear foot of curb installed.  Ram all spaces under the curb so that it is completely supported throughout the entire length.


B.
Butt joint curb sections together.


C.
Install joint sealer as specified in Section 321373 where curb abuts existing walls, posts, buildings, and fixed structures or appurtenances.

EDIT ABOVE AND BELOW TO SUIT PROJECT.
3.02
RESETTING EXISTING CURBS


A.
Remove mortar and concrete from existing curbs to be reused.  Replace units damaged by the contractor’s negligence.


B.
Reset existing curbs approved for reuse by the Director’s Representative.

3.03
FIELD QUALITY CONTROL


A.
The Director may conduct additional tests at their discretion.  Replace curb units taken for testing, not to exceed 10 linear feet for each 1000 feet or fraction thereof delivered to the project.

END OF SECTION

Updated 06/29/2023

Printed 6/29/2023
321614 - 2
Project No. 


